Concrete World Industries

CLEAR CONCRETE SEALER

DESCRIPTION: Concrete World Industries Clear Concrete Sealer is a clear solvent-based acrylic sealer specifically made for universal use on concrete flatwork surfaces and spray-on resurfaced concrete; and, use as a clear base for CWI colour-pigment sealer tint. Since all acrylic sealers will deteriorate in time and from exposure conditions and weathering, no guarantee is or can be given by the manufacturer for serviceability performance, failure from improper workmanship or installation and neglect of maintenance.

RECOMMENDED USE: Internal / external concrete flatwork surfaces and spray-on resurfaced concrete.

FEATURES & BENEFITS:

Excellent bond-strength. Ready-to-use, suitable for DIY. Roll-on or broom-on application. UV Stabilised. Good general surface protection

.

PRECAUTIONS & LIMITATIONS: The Product cannot be installed externally in wet weather or afterwards for a period of at least 48 hours and neither when ambient temperature is outside the range of 5C to 30C. High ambient temperature when combined with strong wind and low humidity risks premature drying and product failure. Efflorescence can occur in finished concrete that may, under certain conditions, migrate to the finished coated surface. No guarantee is or can be given against emergence of efflorescence or other insoluble materials / staining agents that may migrate to or become apparent on the finished coated surface. The Product is not recommended for use on smooth sloping concrete surfaces that include driveways and footpaths in hilly residential or commercial locations or anywhere slip resistance may be compromised when surfaces are wet. Product application must be in accordance with the manufacturer’s approved method to achieve a reasonable probability of serviceability and installers must comply with MSDS & PPE advice for safe use.

# SURFACE PREPARATION & APPLICATION: Attention to surface preparation and installation procedures is essential for proper and workmanlike outcomes of Concrete World Industries Clear Concrete Sealer.

# Important surface preparation & installation procedures are:

- Surface must be free of dirt, dust and contaminants. Efflorescence on concrete surfaces may or will require treatment with a mild hydrochloric acid solution in accordance with recognized method.

- Highly porous surfaces may require two finish coats. If the concrete is ‘new’, apply Concrete World Industries  ‘Prime & Seal’ to aid curing. Wait at least 5-days for ‘new’ concrete to cure before installation of CWI Clear Concrete Sealer.

- Mature concrete surfaces must be ‘primed’ with an initial First Coat of Concrete World Industries Clear ‘Prime & Seal’ to promote bond strength. Apply by broom or roll-on method. Wait at least 24-hours after application of the ‘Primer’ coat before installation of CWI Clear Concrete Sealer.

- Concrete surfaces must be completely and thoroughly dry during product installation. The product must not be applied on moisture or rain affected surfaces. Failure will result. Damp or wet surfaces must be dry at least 48 hours before product installation.

- The completed work must be allowed to cure before exposure to traffic – at least 24 hours for pedestrians; at least 3 days but preferably 7 days for motor vehicles.

Specification:

Application Guide

PRODUCT APPLICATION – IN BRIEF:

Application Instructions Summarised.

Primer Coat: Apply CWI ‘Prime & Seal’ by roll-on method if the concrete is ‘new’. Broom-on mature concrete surfaces so as to ensure good penetration of the primer coat into the slab surface. Important Note: Hard-trowelled internal concrete floor slabs may or will require pre-treatment by sanding or with a mild hydrochloric acid solution to affect proper penetration of the primer coat.

Finish Coat: If the concrete is ‘new’, wait at least 5-days after installation of the primer coat before applying the CWI Clear Concrete Sealer finish coat: If the concrete is ‘mature’, wait at least 24-hours before applying the Finish Coat. Install evenly and uniformly to the surface by roll-on method. Highly porous concrete surfaces may require 2-finish coats to achieve an aesthetically acceptable outcome of the work.

Estimating Coverage: To ensure sufficient and uniform coverage, CWI ‘Prime & Seal’ and CWI Clear Concrete Sealer must be applied at least the minimum recommended rate of 3-4m2 / Litre.

Note: Coverage estimate is a guide only. Variation may or will occur subject to concrete porosity and surface condition, waste factors and scope of the works.

CHEMICAL RESISTANCE: Concrete World Industries Clear Concrete Sealer is resistant to most mild household chemicals. Methylates may or will cause the hard-state sealer to ‘whiten’ and is repairable with Concrete World Industries Solvent. Wipe up spills immediately. CWI Clear and/ or Colour Pigmented concrete sealers are non-resistant if exposed to petrochemicals or similarly corrosive liquids or powders that require purpose-made paints or sealer coatings.

PACKAGING & STORAGE: Concrete World Industries Sealer products are packaged in 20- litre pails and must be stored undercover, above ground and protected from the elements. Shelf life is at least 12 months from date of manufacture subject to climate and storage conditions. Avoid exposure to direct heat & flame sources. Flammable Liquid. Hazchem Code: 3[Y]

PRODUCT USE WARNING: CWI Clear Concrete Sealer is not suitable for use on clay-based pavers or natural masonry surfaces. The product is not designed for use as a waterproofing agent. It is the user’s responsibility to make determination of the safety and suitability of product use for particular projects. No warranty expressed or implied is given for product misuse, property damage or personal injury.

# IMPORTANT NOTE:

The information provided in this publication is for general guidance only. Concrete World Industries Pty Ltd accepts no liability for its use. Workmanship and product application in accordance with product specifications, precautions and limitations is the responsibility of the tradesperson contracted to carry out the work. Warranty is strictly limited to proven defective or faulty product supplied at the point of sale.

Concrete World Industries

106 Fitzroy Street Dubbo

www.cwid.com.au

admin@cwid.com.au

(02) 6885 6876